## Slide 1
AP6180/AP8180:
Modern Scattering Methods in Materials Science
Lecture given by Prof. Tamas UNGAR
Office: G6601
E-mail: tungar@cityu.edu.hk
Course leader: Dr Suresh M. Chathoth
Application of the Kinematical Scattering to
Solve Problems in Materials Science

## Slide 2
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 3
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 4
Atoms (molecules) pack together in a regular pattern to form a crystal.
There are two aspects to this pattern:
    Periodicity
    Symmetry
First, consider the periodicity…
Little crystallography
James A. Kaduc, Crystallography lecture

## Slide 5: A Primitive Cubic Lattice (CsCl)
Little crystallography
James A. Kaduc, Crystallography lecture

## Slide 6
a unit cell of a lattice (or crystal) is a volume which can describe the lattice using only translations.
in 3 dimensions (for crystallographers), this volume is a parallelepiped.
such a volume can be defined by six numbers
- the lengths of the three sides,
or three basis vectors
- and the angles between them
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: I like the word “parallelepiped”.
we’ll see more about basis vectors later

## Slide 7
Little crystallography: lattice vectors and angles
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 8
the unit cell is not unique
(c:\MyFiles\Clinic\index2.wrl)
Little crystallography
James A. Kaduc, Crystallography lecture

## Slide 9
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: Convenient and necessary to have symmetry elements at corners/edges/faces
Not the box

## Slide 10
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: Different cells – trigonal/orthorhombic, emphasize same points at corners

## Slide 11
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: Higher metric symmetry?

## Slide 12
how to pick the unit cell?
axis must be right-handed
angles should be close to 90°
periodicity plus symmetry
has to be fulfilled at the same time
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: Symmetry makes life easier, and the problems smaller
Both senses of orthogonal – 90 deg and lower correlations
The rules sometimes conflict – pick best for your purposes, and get ready to argue with referees!

## Slide 13
Little crystallography: lattices
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 14
Little crystallography: lattices
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 15
Little crystallography: the unit-cell
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 16
one-fold “1” two-fold “2” three-fold “3” four-fold “4” axis
six-fould “6” mirror-plane “m” mirror plus mirror plus
axis two-fold axis four-fold axis
Little crystallography: symmetry operators
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 17
a tetrahedron can be placed in
12 distinct positions by
rotation alone
the 12 rotations form the rotation group
group of symmetry operations
of the tetrahedron
symmetry group: group of symmetry operations

## Slide 18
Point Group
a crystallographic point group is
a set of symmetry operations, like rotations or reflections,
that leave a central point fixed while moving
other directions and faces of the crystal
to the positions of features of the same kind
point groups must comply with translational symmetry
there exist 32 point-groups

## Slide 19
Schoenflies notation
Cn (c:cyclic): n-fold rotation axis
S2n (s:piegel=mirror) 2n-fold rotation-reflection axis
Dn (d:dihedral=two-sided) n-fold rotation axis
plus n twofold axes perpendicular to that axis
T (tetrahedron) symmetry of a tetrahedron
O (octahedron) symmetry of an octahedron or cube

## Slide 20
Space Group
crystallographic space groups are
the crystallographic or Fedorov groups,
of consecutive symmetry operations
describing the symmetry of a crystal
there are 230 space-groups

## Slide 21: Symmetry information is tabulated in International Tables for Crystallography, Volume A edited by Theo Hahn Fifth Edition 2002
Little crystallography
James A. Kaduc, Crystallography lecture
Notes: You simply have to have one (or more) of your own!

## Slide 22: Guaifenesin, P212121 (#19)
Little crystallography: “spacegroup” notation
James A. Kaduc, Crystallography lecture

## Slide 23
P212121 (#19) P: simple
21: two-fold screw-axis
orthorhombic Bravais lattices
Little crystallography: “spacegroup” notation
21 is a 180°, twofold rotation followed by a translation of ½ of the lattice vector,
31 is a 120°, threefold rotation followed by a translation of ⅓ of the lattice vector.
Guaifenesin: also glyceryl guaiacolate,
an expectorant drug sold over the counter
usually taken orally to assist the bringing up (expectoration) of
phlegm from the airways in acute respiratory tract infections

## Slide 24
Little crystallography: Bravais lattices
 space-groups can be sorted into 14 symmetry groups
 these form 7 crystal systems
 the spatial forms of the 14 symmetry groups
are the Bravais lattices
 the Bravais lattices are the conceivable unit-cells
which comply with:
translational symmetry and crystal symmetry
at the same time

## Slide 25
Little crystallography: Bravais lattices
space groups (#)
195-230
75-142
16-74
168-194
143167
3-15
1-2

## Slide 26
Little crystallography: Bravais lattices
(trigonal)
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 27
Little crystallography: Bravais lattices
once again

## Slide 28
Little crystallography
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 29
Little crystallography
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 30
Little crystallography
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 31
Little crystallography: lattice-planes in two dimensions
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 32
Miller indices
intercepts of the lattice plane:
a, b/2, 3c: 1, ½, 3
reciprocals of the intercepts:
1, 2, 1/3
the smallest integers of the same ratio:
1:2:1/3 = 3:6:1
3,6,1: are the Miller indices of the plane
general denotation: h,k,l

## Slide 33
properties of the Miller indices
cubic

z
y
x
cos = =
cos =
cos =
= 1 = (h2 + k2 + l2)
d =

## Slide 34
properties of the Miller indices
lattice plane:
goes through the lattice points
n: normal vector of the lattice plane
n = ha1 + ka2 +la3

## Slide 35
distance formulas for different lattices

## Slide 36
reciprocal lattice
reciprocal space:
reciprocal-space vector: g
g = hb1 + kb2 + lb3
ng = h2 + k2 + l2

## Slide 37
Little crystallography
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
crystal lattice reciprocal lattice

## Slide 38
Little crystallography
theorem #1:
g is perpendicular to the hkl crystal-plane
g = hb1 + kb2 + lb3
z
y
x
is a vector in the plane
g = 0

## Slide 39
Little crystallography
theorem #2:
ghkl =
for cubic crystals:
g = b
g = b = =
d =

## Slide 40
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 41
equations of Laue
a1
-s0a1
sa1
difference of path for
intensity maxima:
a1s – a1s0 = n1
a1(s – s0) = n1
a2(s – s0) = n2
a3(s – s0) = n3
the equations
of Laue

## Slide 42
equations of Laue
a1(k – k0) = n1
a2(k – k0) = n2
a3(k – k0) = n3
s = k
theorem #3:
ni are integers
this can only be satisfied if and only if:
k - k0 is a reciprocal-space vector:
k - k0 = g = n1b1+ n2b2+ n3b3

## Slide 43
Bragg’s law of scattering
2
k0
k
g
lattice planes
g = = k-k0 =
 = 2 d sin

## Slide 44
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
physical meaning of extinction length,
Debye’s equation of diffraction,
Incorporating the unit cell and translational symmetry,
Structure factor,
Patterson function,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 45
kinematical vs. dynamical scattering
lattice planes in a large crystal
and perfect
crystal surface
incident beam
scattering is
back & forth
energy travels
parallel to
the planes
energy

## Slide 46
kinematical vs. dynamical scattering
lattice planes in a small crystal
crystal surface
incident beam
scattering occurs
one single times

## Slide 47
kinematical vs. dynamical scattering
we want to deal with small crystals
where scattering occurs one single times:
this is: kinematical scattering

## Slide 48
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Patterson function,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 49
a1
a3
a2
Rmn
r2
m1a1+m2a2+m3a3
N2
N1
Rmn = m1a1+m2a2+m3a3+rn
scattering by a small crystal

## Slide 50
By introducing the elementary-cell:
translational symmetry is taken care of
scattering by a small crystal

## Slide 51
The X-ray beam is: a plane wave (Fraunhofer conditions)

so
s
R
Rmn
x1
P
position of observation
x2
x2’
O
incoming plane wave
scattering by a small crystal
Warren, X-ray Diffraction

## Slide 52
Electromagnetic field at P
P = fn
x1 = so Rmn
x2 = R – s Rmn x2  x2’
x1 + x2 = R – (s - so)Rmn
P = fn
scattering by a small crystal
Warren, X-ray Diffraction

## Slide 53
This has to be summed up for all atoms
within the
1) molecules
2) the “basis”
consisting of molecules
3) the “nodes” of the space group
consisting of basis and molecules
i.e. for all n and m indices
scattering by a small crystal
P = fn
Warren, X-ray Diffraction

## Slide 54
scattering by a small crystal
four summation terms: n, m1, m2, m3,




Warren, X-ray Diffraction

## Slide 55
scattering by a small crystal
the first term:
is NOT affected by the structure
Warren, X-ray Diffraction

## Slide 56
scattering by a small crystal
the three terms with: m1, m2, m3: are equivalent with the
Laue equations:
Warren, X-ray Diffraction

## Slide 57
the three terms with: m1, m2, m3 have the form of a geometric series:
using this relation:
for all three sums over mi:
the intensity is the squared absolute value of the amplitude:
this will have the form:
scattering by a small crystal
Warren, X-ray Diffraction

## Slide 58
scattering by a small crystal
the function has
the form for N=20:
it can be shown that:
lim = (x)
N
the maxima are at: r(k-k0) = integers
just as in the Laue equations
(or 2integers)
Warren, X-ray Diffraction

## Slide 59
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 60
now we turn to the term:
this contains rn, the positions of the atoms in the unit-cell
the aim of the diffraction experiment is to determine the rn values,
i.e. the positions of the atoms in the structure,
the term above gives the rn values:
we call this term the structure factor: F or Fhkl
scattering by a small crystal
Warren, X-ray Diffraction

## Slide 61
the structure factor
F =
in a Bragg maximum, at ghkl, the expression
must be a reciprocal lattice vector, i.e.
= ghkl = hb1+kb2+lb3
rn is a lattice vector: rn = x1a1+x2a2+x3a3
ghklrn = hxn+kyn+lzn, thus
Fhkl =

## Slide 62
the structure factor
structure factor for a simple fcc crystal:
(0,0,0,)
(1/2,1/2,0)
(0,1/2,1/2)
(1/2,0,1/2)
Fhkl = (e2i(0)+e2i(h+k)+e2i(h+l)+e2i(k+l))
if hkl all even: 1 1 1 1
if hkl all odd: 1 1 1 1
if hkl mixed parity: e.g. 1 -1 -1 1

## Slide 63
the structure factor
structure factor for a simple fcc crystal:
(0,0,0,)
(1/2,1/2,0)
(0,1/2,1/2)
(1/2,0,1/2)
1 0 0 missing
1 1 0 missing
1 1 1
2 0 0
2 1 0 missing
2 1 1 missing
2 2 0
2 2 1 missing
2 2 2
3 0 0 missing
3 1 0 missing
3 1 1
.
.
systematic extinction

## Slide 64
systematic extinction

## Slide 65
Debye-Scherrer powder patterns

## Slide 66
the structure factor
structure factor for a crystal with the
fcc Bravais lattice:
or:
Warren, X-ray Diffraction

## Slide 67
the structure factor
structure factor for a crystal with the
bcc Bravais lattice:
or:
Warren, X-ray Diffraction

## Slide 68
in
either Cl or Na can be used for evaluationg the “group”,
let (000) be for Cl and (1/2,1/2,1/2) for Na: the group
this yields:
finally:
the structure factor for NaCl
Warren, X-ray Diffraction

## Slide 69
in
either Cl or Na can be used for evaluationg the “group”,
let (000) be for Zn and (1/4,1/4,1/4) for S: the group
this yields:
finally:
the structure factor for ZnS (zink-blend)
Warren, X-ray Diffraction

## Slide 70
in
we can use the ZnS result
finally:
the structure factor for diamond
Warren, X-ray Diffraction
C1
C2
0, missing

## Slide 71
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 72
Ewald construction
the graphical representation of Bragg’s law

## Slide 73
the graphical representation of Bragg’s law
2
k0
k, k=
g
lattice planes
g = = k-k0 =
 = 2 d sin
Ewald construction

## Slide 74

2
k0
k, k=
g
lattice planes
Ewald construction
           
           
           
           
           
r =1/

O
hkl “excited”
reciprocal lattice
whenever the Ewald sphere
goes through a reciprocal lattice-point
the corresponding hkl reflection
will be “excited”
beware of “systematic extinction”

## Slide 75
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 76
Powder diffraction (I)
2
k0
k
g
in a polycrystal or “powder” specimen
the same set of lattice planes occur in
many orientations, each corresponding to
a different crystal in the sample


Ewald sphere
polycrystal sphere

## Slide 77
Powder diffraction (I)
2
k0
k
g
in a polycrystal or “powder” specimen
the same set of lattice planes occur in
many orientations, each corresponding to
a different crystal in the sample


Ewald sphere
polycrystal sphere
Diffraction cone
Debye-Scherrer line
2

## Slide 78
Powder diffraction (I)
diffraction cones

## Slide 79
Debye-Scherrer geometry

## Slide 80
Debye-Scherrer geometry
Debye-Scherrer line
base-line of the
diffraction-cone
detector
collimator
specimen
the geometry of each
parallel beam
diffractometer

## Slide 81
line-focus point-focus in the lab
point
 6o
line
tungsten filament

## Slide 82
Bragg-Brentano parafocusing geometry
the principle

## Slide 83
Bragg-Brentano parafocusing geometry

## Slide 84
Bragg-Brentano parafocusing geometry
 -  arrangement  - 2 geometry

## Slide 85
technical of the parafocusing geometry

## Slide 86
the pyrolytic-graphite monochromator

## Slide 87
X-ray monochromators for lab equipment
curved curved plus ground

## Slide 88
X-ray monochromators for lab equipment
pyrolytic carbon:  100 m crystallite size
 1o mosaicity
large receiving angle
relatively large bandwidth, /0.01
secondary, reflected-beam monochrom.
reduces background
reduces fluorescent contribution

## Slide 89
primary-beam X-ray monochromators

## Slide 90
Guinier focusing camera

## Slide 91
Guinier focusing camera
forward
backward
reflection

## Slide 92
Göbel mirror

## Slide 93
in more detail:
Little crystallography
Bragg’s law of scattering,
Kinematical versus dynamical scattering,
Physical meaning of extinction length,
Scattering by a small crystal,
Incorporating the unit cell and translational symmetry,
Structure factor,
Ewald construction in reciprocal space,
Fundamental equipment for
X-ray diffraction experiments,
Diffractometers and detectors

## Slide 94
-2 diffractometer designed by Parrish in the 1940’s
never surpassed

## Slide 95
-2 diffractometer designed by Parrish in the 1940’s
with primary-beam-monochromator

## Slide 96
X-ray detectors
CCD

## Slide 97
X-ray detectors
GE amorphous silicon
 400 mm
MAR imaging-plate

## Slide 98
X-ray detectors
“strip” detectors

## Slide 99
Thank you