## Slide 1
A6180/8180:
Modern Scattering Methods in Materials Science
Lecture given by Prof. Tamas UNGAR
Office: G6601
E-mail: tungar@cityu.edu.hk
Course leader: Dr Suresh M. Chathoth
Scattering by non-crystalline materials
Debye-formula
Zernicke-Prins equation

## Slide 2
the scattered intensity in the most general form:
where summation has to be done over all the atoms within the illuminated region,
with the difference vector rmn = rm – rn :
Warren, X-ray Diffraction

## Slide 3
Warren, X-ray Diffraction

## Slide 4
with , the average for each exponential term:
=
=
=
after summation
Debye-formula
Warren, X-ray Diffraction

## Slide 5
gas of polyatomic molecule:
where the last term on the right-hand side if the modified Compton scattering
and N is the number of molecules in the illuminated volume.
Warren, X-ray Diffraction

## Slide 6
carbon-tetrachloride CCl4:
+
+
Warren, X-ray Diffraction

## Slide 7
Warren, X-ray Diffraction

## Slide 8
rC-Cl = 0.182 nm

## Slide 9
Scattering by liquid or non-crystalline materials
if there is only one kind of atom, the scattered intensity will be:
we introduce a density function:
where is the number of atoms in dVn at rnm.
With this the summation can be replaced by the integral:
Warren, X-ray Diffraction

## Slide 10
Scattering by liquid or non-crystalline materials
with introducing the average density, a:
+
for a fixed distance rmn=r let , where the average
is over all m(r) within the sample at the distance r from any atom
in the sample.
Warren, X-ray Diffraction

## Slide 11
Scattering by liquid or non-crystalline materials
for a fixed distance in the sample,
where the average is taken over all m(r) within the sample
at the distance r from any atom.
With this, in the integral can be replaced by:
Warren, X-ray Diffraction

## Slide 12
Scattering by liquid or non-crystalline materials
For a mon-atomic amorphous sample the term
goes to zero at distances of r larger than a few atomic distances.
Since the volume S is considerably larger than a few atomic distances
the summation over m can be replaced
by the number of atoms in S, i.e., N.
Warren, X-ray Diffraction

## Slide 13
Scattering by liquid or non-crystalline materials
if there is no preferred orientation in the sample,
will have spherical symmetry and can be written as:
Warren, X-ray Diffraction

## Slide 14
Scattering by liquid or non-crystalline materials
if there is no preferred orientation in the sample,
will have spherical symmetry and can be written as:
Using the notations in Fig. 10.1 and the variable
we obtain:
=
Warren, X-ray Diffraction

## Slide 15
Scattering by liquid or non-crystalline materials
Warren, X-ray Diffraction

## Slide 16
Scattering by liquid or non-crystalline materials
after some rearrangements:
+
next we analyze the integral in the third term:
Warren, X-ray Diffraction

## Slide 17
Scattering by liquid or non-crystalline materials
since a is a constant, the integral can be written as:
dVn
the integral here is the Fourier transform of the form-factor
of the volume of the sample within S. If S is macroscopic
then the integral is close to a delta function around the
direct-beam direction, and therefore has no effect on
the diffraction experiment.
The third term on the right-hand site of Ieu can be omitted.
Warren, X-ray Diffraction

## Slide 18
Scattering by liquid or non-crystalline materials
the scattered intensity per atom will become:
We introduce the abbreviation:
,
and do some rearrangements:
Warren, X-ray Diffraction

## Slide 19
Scattering by liquid or non-crystalline materials
with taking into account the rules of Fourier transformation:
the inverse Fourier transformation provides:
and with some rearrangements:
Warren, X-ray Diffraction

## Slide 20
Scattering by liquid or non-crystalline materials
we arrive at the Zernicke-Prins equation:
4r2(r) is the radial-distribution-function (RDF)
Warren, X-ray Diffraction

## Slide 21
Scattering by liquid or non-crystalline materials
Warren, X-ray Diffraction

## Slide 22
Scattering by liquid or non-crystalline materials
Warren, X-ray Diffraction

## Slide 23
Scattering by liquid or non-crystalline materials
Warren, X-ray Diffraction

## Slide 24
Thank you