## Slide 1
AP6180/AP8180
Modern Scattering Methods in Materials Science
Lecture given by Prof. Tamas UNGAR
Office: G6601
e-mail: tungar@cityu.edu.hk
Course leader: Dr Suresh M. Chathoth
Fundamentals of X-ray scattering

## Slide 2
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 3
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 4
Brief history
Reading:
B.E.Warren, X-ray Diffraction,
Dover Publ., 1969, 1990
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
Prentice Hall Inc. 2001
P.Klug & L.E.Alexander, X-ray diffraction procedures
for polycrystalline and amorphous materials,
Wiley, NY, 1954
L.H.Schwartz & J.B.Cohen, Diffraction from Materials,
AP. Academic Press, 1977

## Slide 5
The tale:
Röntgen, a German physicist,
was experimenting with a Crookes tube
when it produced streams of electrons
called cathode rays.
Just before leaving for lunch one day,
Röntgen put an activated tube on a book and
the book just happened to be lying on
a piece of photographic film.
Inside the book was a key and
when he later discovered that image,
he knew he was looking at
something entriely new.
The world's first ever x-ray
Discovery: 1895, Nobel Prize: 1901
Wilhelm Konrad Röntgen
1845 - 1923

## Slide 6
Crookes tube

## Slide 7
X-ray or röntgen image of
one of the hands of
Röntgen’s wife

## Slide 8
the first diffraction experiments: Max von Laue, 1912
Laue photograph of zinc blend, ZnS
along the three-fold axis
M.vonLaue, Friedrich & Knipping, 1912

## Slide 9
the first diffraction experiments: Max von Laue, 1912
third improved image,
after applying a pinhole
Laue photograph of zinc-blend, ZnS
along the three-fold axis
M.vonLaue, Friedrich & Knipping, 1912

## Slide 10
the first diffraction experiments: Max von Laue, 1912

## Slide 11
the first diffraction experiments: Max von Laue, 1912
two consequences
1) materials are crystalline consisting of atoms
2) X-rays are waves
electromagnetic waves
Nobel Prize in Physics 1914

## Slide 12
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 13
the first X-ray tubes:

## Slide 14
the first X-ray tubes:

## Slide 15
X-ray tubes today

## Slide 16
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 17
X-ray spectra
bremsstrahlung radiation produced by
random inelastic scattering by
the electrons in the material

## Slide 18
X-ray spectra
characteristic X-ray spectrum radiation produced by
when the exited atom relaxes
by emitting a photon

## Slide 19
X-ray spectra
characteristic
X-ray spectrum
radiation produced by
when the exited atom relaxes
by emitting a photon

## Slide 20
X-ray spectra

## Slide 21
X-ray spectra

## Slide 22
X-ray wavelengths used in the laboratory

## Slide 23
X-ray spectra

## Slide 24
X-ray spectra

## Slide 25
X-ray spectra

## Slide 26
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 27
X-ray absorption
dx
I(x) I(x+dx)
= = -dx
Ix = Ioe-x = Ioe-(/)x
/ : mass-absorption coefficient
/ = k 3 Z3 between absorption edges

## Slide 28
X-ray absorption spectrum for platinum
I = Ioe-x = Ioe-(/)x / : mass-absorption coefficient

## Slide 29
X-ray absorption
                cm2/g
Warren, X-ray diffraction

## Slide 30
X-ray absorption
                cm2/g
Warren, X-ray diffraction

## Slide 31
X-ray absorption
                cm2/g
Warren, X-ray diffraction

## Slide 32
X-ray filters

## Slide 33
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 34
correspondence between different radiations

## Slide 35
correspondence between different radiations

## Slide 36
solving the acronyms
LEED: low energy electron diffraction
AES: Auger electron scattering
EELS: electron energy loss spectroscopy
SEM: scanning electron microscopy
HEED: high energy electron diffraction
TEM: transmission electron microscopy
XRD: X-ray diffraction
Cold/thermal: thermalized neutrons
XPS: X-ray-photon-spectroscopy
Synchrotron: synchrotron source of photons

## Slide 37
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 38
The first ”synchrotron source”
“Synchrotron radiation was seen for the first time at the
General Electric in the USA in 1947”

## Slide 39
Brilliance of X-ray sources:
number of fotons
sec × mm2

## Slide 40
foton/s/mm2
1034
1024
1012
108
120 years of
brilliance

## Slide 41
Synchrotron X-ray sources
X-ray beam
packages of electrons

## Slide 42
ESRF, Grenoble
European Synchrotron Radiation Facility
ILL

## Slide 43
ESRF, Grenoble
European Synchrotron Radiation Facility

## Slide 44
ID31
high resolution
powder diffractometer
 3 m

## Slide 45
ID31 high resolution powder diffractometer:
detector system

## Slide 46
protein crystallography
X-ray beam

## Slide 47
ESRF, Grenoble
European Synchrotron Radiation Facility
protein crystallography

## Slide 48
ESRF, Grenoble
European Synchrotron Radiation Facility
protein crystallography

## Slide 49
protein crystallography

## Slide 50
APS, Argonne, IL, USA
Advanced Photon Source

## Slide 51
SPring-8
Japan’s synchrotron

## Slide 52
SPring-8
Japan’s synchrotron

## Slide 53
incertion devices
  Bending magnet
  Wiggler
  Undulator
controlling the path of electrons

## Slide 54
Bending magnet

## Slide 55
Wiggler
Intensities are adding up

## Slide 56
Undulator
the amplitudes are in phase

## Slide 57
typical undulator spectrum at APS - Argonne

## Slide 58
X-ray spectra at
SPring-8

## Slide 59
free electron laser: FEL
a very long undulator

## Slide 60
the synchrotron in Hamburg (Germany) today:

## Slide 61
schematics of the European Free Electron Laser (XFEL)
3,2 km

## Slide 62
Vizsgáló sugárzások
Vizsgálat tárgyai
courtecy: Hastings, Stanford

## Slide 63
prospective diffraction on
single molecules
at the European FEL

## Slide 64
courtecy: Hajdu, Uppsala

## Slide 65
courtecy: Hajdu, Uppsala

## Slide 66
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 67

E

-
+
-
+
the polarized dipole radiates
the atom is polarized
Mechanism of X-ray scattering

## Slide 68
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 69
scattering of X-rays by an electron
s0
s
Warren, X-ray diffraction
the electric field, , in cgs units:

## Slide 70
Warren, X-ray diffraction
the Y’ component of the electric field at P:
the amplitude is:
the E0Z amplitude (for the EZ =90o) :
Y
E0Y’
scattering of X-rays by an electron

## Slide 71
Warren, X-ray diffraction
the observed intensity at P:
assuming that the incoming beam is randomly polarized:
and
finally:
polarization factor
for an unpolarized
incoming beam
scattering of X-rays by an electron

## Slide 72
Warren, X-ray diffraction
the numerical factor in the scattered intensity:
the number of electrons in the volume illuminated by the incoming beam
in a usual specimen:
 1022
therefore, the scattered intensity is approximately of-the-order of:
Iscattered  I0  10-4
scattering of X-rays by an electron

## Slide 73
scattering of X-rays by an atom
rn is the position of the n-th electron
in the atom
Warren, X-ray diffraction
the amplitude scattered by the n-th electron at P:
X1 << X2
it can be shown that:

## Slide 74
scattering of X-rays by an atom
Warren, X-ray diffraction
turning to complex exponentials and summing over all electrons:
e
electron scattering factor, fe
 is the average charge-density distribution
of the electron
fe is the amplitude scattered by an electron in 1-electron-scattering-units
scattering of X-rays by a smeared-out electron

## Slide 75
Warren, X-ray diffraction
scattering of X-rays by a smeared-out electron
taking into account the real charge-density distribution:  (r)
the atomic scattering-factor:
f is measured in units of
scattering by a single electron
scattering of X-rays by an atom

## Slide 76
atomic scattering factors of X-rays
Klug & Alexander, X-ray diffraction

## Slide 77
atomic scattering factors of X-rays
Klug & Alexander, X-ray diffraction

## Slide 78
atomic scattering factors of X-rays
at k=0, where k=4sin/, sinkr/kr = 1,
i.e. in the forward scattering case, or at small values of 2:
Warren, X-ray diffraction

## Slide 79
comparison of scattering factors of X-rays and neutrons
scattering factors/lengths

## Slide 80
comparison of scattering factors of X-rays and neutrons
q or angle dependence of scattering factor

## Slide 81
comparison of scattering factors of X-rays and neutrons

## Slide 82
Fundamentals of X-ray scattering
Brief history
Laboratory X-ray sources,
Basic properties of X-rays,
X-ray spectra,
X-ray absorption edges,
Synchrotron X-ray sources,
Scattering mechanisms of X-rays by matter,
Atomic scattering factors for X-rays
Total X-ray reflection,
Darwin-breadth (qualitatively)
Monochromators (briefly)

## Slide 83
kinematical vs. dynamical scattering
lattice planes in a large crystal
and perfect
crystal surface
incident beam
scattering is
back & forth
energy travels
parallel to
the planes
energy

## Slide 84
kinematical vs. dynamical scattering
lattice planes in a small crystal
crystal surface
incident beam
scattering occurs
one single times

## Slide 85
kinematical vs. dynamical scattering
we want to deal with small crystals
where scattering occurs one single times:
this is: kinematical scattering

## Slide 86
kinematical vs. dynamical scattering
monochromators are large perfect crystal
scattering occurs in the
dynamical regime
Darwin breadth
Cu (200): 19’’
Si (220): 5.02’’
http://www.chess.cornell.edu/oldchess/operatns/xrclcdwn.htm

## Slide 87
Thank you