## Slide 1
A6180/8180:
Modern Scattering Methods in Materials Science
Lecture given by Prof. Tamas UNGAR
Office: G6601
E-mail: tungar@cityu.edu.hk
Course leader: Dr Suresh M. Chathoth
Structure determination by diffraction

## Slide 2
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 3
indexing
20
Warren, X-ray Diffraction

## Slide 4
indexing
Warren, X-ray Diffraction

## Slide 5
indexing
Warren, X-ray Diffraction
divide #2 by 0.0940
divide #2 by
divide #2 by
etc.

## Slide 6
indexing
Warren, X-ray Diffraction
column #3 from #2
3
4.0053
8.02978
11.0265
12.0255
16.053
19.085
20.0744
24.0957
27.0957

## Slide 7
Warren, X-ray Diffraction
indexing and structure from a powder pattern

## Slide 8
Warren, X-ray Diffraction
columns #7 and #8
Na 11
Cl 17
indexing and structure from a powder pattern

## Slide 9
indexing and structure from a powder pattern
Warren, X-ray Diffraction
column #9
M: Na Cl
we can choose the coordinates of the 4 Cl atoms as:
where to put the Na atoms?
if one Na is at: x,y,z, then the other 3 are fixed
for the first position there are 3 possibilities in a cubic lattice:
but only the first 2 are different
we can start with the first option:

## Slide 10
Warren, X-ray Diffraction
LP : Lorentz-Polarization factor
polarization factor
Lorentz - polarization factor
for an unpolarized incoming beam
indexing and structure from a powder pattern

## Slide 11
indexing NaCl as ZnS
the intensities turn out to be wrong
Warren, X-ray Diffraction
indexing and structure from a powder pattern
from the two options:
checking with the other option:

## Slide 12
Na Cl ZnS
indexing and structure from a powder pattern

## Slide 13
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 14
the structure factor in terms of continuous electron/charge density:
this is a Fourier transform:
Fhkl = FT[(r)]
The scattered intensity: I(K) = Fhkl 2, where K =
Patterson function

## Slide 15
Fhkl 2 = Fhkl  Fhkl* = FT[(r)]×FT[(-r)] =
= FT[(r)  (-r)] = FT[P(r)]
P(r) =
Patterson function: autocorrelation of (r)
Patterson function

## Slide 16
Patterson function
linear charge density and the corresponding Patterson function

## Slide 17
Patterson function
a diffraction experiment yields: the pair - correlation

## Slide 18
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 19
phase analysis, data – bases
a diffraction pattern is the fingerprint of materials

## Slide 20
phase analysis, data – bases
a diffraction pattern is the fingerprint of materials

## Slide 21
ICDD data files

## Slide 22
ICDD data files

## Slide 23
ICDD data files

## Slide 24
ICDD data files

## Slide 25
ICDD data files

## Slide 26
ICDD data files

## Slide 27
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 28
the Rietveld method
structure refinement from powder patterns
the principle of the Rietveld Method is
to minimize a function M, the difference between
the measured diffraction pattern yobs
and the calculated pattern ycalc
Wi : weights, c : scaling factor

## Slide 29
the Rietveld method

## Slide 30
the Rietveld method

## Slide 31
the Rietveld method
R.A.Jung: The Rietveld Method, 1993

## Slide 32
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 33
Macherauch, E. (1965)
schematic classification of internal stresses

## Slide 34
Macherauch, E. (1965)
schematic classification of internal stresses
I: macro-stress
averaged over many grains
II: intergranular-stresses
averaged over individual grains
III: micro-strains (or stresses)
produced by dislocations

## Slide 35
stress – strain
ONLY strain can be measured
d
d
d

## Slide 36
stress – strain
ONLY strain can be measured
d is always measured
parallel to g
where d is the distance of the
planes normal to the
g vector
tilting the specimen allows to
determine different components
of the strain-tensor
d
d
d

## Slide 37
stress – strain
the 6-circle diffractometer
for stress measurement
at synchrotrons
http://www.opengda.org/documentation/manuals/Diffcalc/trunk/user/manual.html

## Slide 38
stress – strain
usual notations for X-ray
stress-strain experiments
S1, S2, S3 : sample coordinates
L1, L2, L3 : laboratory coordinates

## Slide 39
stress – strain
g

n

## Slide 40
stress – strain
sample coordinates
laboratory coordinates
(1)

## Slide 41
stress – strain
(a)
typical plots
a, b : eq. (1) can be solved
c : eq. (1) cannot be solved
(c)
(b)

## Slide 42
Detector Bank #2
+90°
Detector Bank #1 -90°
Q1
Q2
lattice – strains
time-of-flight (TOF)
neutron beam

## Slide 43: Detector Banks + Collimators VULCAN, SNS, Oak Ridge
lattice – strains

## Slide 44
lattice – strains
B1
axial
B2
side

316 stainless-steel

## Slide 45
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 46
texture
bulk, polycrystalline materials
consist almost
NEVER
of randomly oriented
grains or crystallites
the distribution of the
crystallographic orientation of
grains or crystallites is
TEXTURE

## Slide 47
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
random preferred orientation

## Slide 48
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
54.7o

## Slide 49
texture
[001]
[111]
n
2111

## Slide 50
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 51
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
specimen is rotated over
two axes

## Slide 52
texture
brass-texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 53
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction

## Slide 54
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
orientation-distribution-function (ODF)

## Slide 55
texture
B.D.Cullity & S.R.Stock, Elements of X-ray Diffraction
ODF
cold-rolled brass

## Slide 56
Structure determination by diffraction,
powder diffraction,
systematic extinction,
indexing,
Patterson function
phase analysis,
data-bases and applications,
Rietveld analysis,
special applications,
stress-strain
texture determination,
line profile analysis

## Slide 57
Macherauch, E. (1965)
schematic classification of internal stresses
I: macro-stress
averaged over many grains
II: intergranular-stresses
averaged over individual grains
III: micro-strains (or stresses)
produced by dislocations
+ other effects

## Slide 58
Line broadening is small

## Slide 59
Ni ball-milled for 12 hours
P. Scardi M. Leoni, Acta Cryst. (2002). A58, 190-200
Logarithmic intensity scale

## Slide 60
Al-3 wt% Mg ball-milled for 6 hours
G. Ribárik, J. Gubicza, T. Ungár, Mater. Sci. Eng. A, 387-389 (2004) 343-347.
Logarithmic intensity scale

## Slide 61
ZK60 Mg alloy deformed by ECAP
L. Balogh, R.B. Figueiredo, T. Ungár, T.G. Langdon, Mater. Sci. Eng. A, 528 (2010) 533-538.

## Slide 62
Al-base Al-Mg alloy friction-stir-welded (FSW)
W. Woo, L. Balogh, T. Ungár, H. Choo, Z. Feng, Mater. Sci. Eng. A, 498 (2008) 308-313.

## Slide 63
Al-base Al-Mg alloy friction-stir-welded (FSW)
W. Woo, L. Balogh, T. Ungár, H. Choo, Z. Feng, Mater. Sci. Eng. A, 498 (2008) 308-313.

## Slide 64
Fortunately the instrumental effect
- can be small
- can be corrected, if necessary

## Slide 65
Diffraction from „perfect” crystals of LaB6
ESRF - Grenoble

## Slide 66
Diffraction from PbS - Galena, grinded for 12 hours
T. Ungár, P. Martinetto, G. Ribárik, E. Dooryhée, Ph. Walter, M. Anne, J. Appl. Phys. 91 (2002) 2455-2465.
ESRF - Grenoble

## Slide 67
The difference betwee the Measured and the Instrumental profiles
tells us the microstructure

## Slide 68
X-ray diffraction peaks can
 be shifted
 can become asymmetric
 can broaden
 can have any combination of these three

## Slide 69
[001] Cu single crystals deformed in tension
T.Ungár, H.Mughrabi, D.Roennpagel, M.Wilkens, Acta Metall. 32 (1984) 333.
H.Mughrabi, T.Ungár, W.Kienle M.Wilkens, Phil. Mag. 53 (1986) 793.
(i) broadening:
dislocations
(ii) asymmetry:
internal stresses
gradient stresses
(iii) shift:
homogeneous strains
due to vacancies
(iv) background
has been subtracted

## Slide 70
Peak shifts
internal stresses of different kinds
stacking faults,
chemical inhomogeneities
Broadening
microstrains
nanograins
subgrains
small crystallites
Asymmetries
internal stresses of different kinds
stacking faults,
chemical inhomogeneities

## Slide 71
Separation of the different effects is based on
- order dependence
- hkl anisotropy
- profile-shape
- sub-profile displacement

## Slide 72
. . . . . .
. . . . . .
. . . . . .
. . . . . .
O
Size broadening
Strain broadening
Twinning or faulting
Schematic picture of line broadening

## Slide 73
Two different approaches - philosophies:
top-down
bottom-up

## Slide 74
Top-down:
the diffraction patterns are
fitted by analytical profile-functions
Bottom-up:
the profile-functions are
created by theoretical methods
based on actual lattice defects
diffraction patterns are fitted by
these defect-related profile-functions

## Slide 75
Top-down analytical profile-functions:

## Slide 76
For many good reasons we follow the
bottom-up approach

## Slide 77
The hierarchy of
non-size-type
lattice defects

## Slide 78
0 dimensional: point defects
point-defect-type, e.g. precipitates
inclusions
(r)  1/r2
2 dimensional: planar defects, e.g. stacking faults
twin boundaries
grain boundaries
domain boundaries
(r)  constant
1 dimensional: dislocations
non-equilibrium triple-junctions
linear-type defects
(r)  1/r
Krivoglaz: the spatial dependence of strain: (r)

## Slide 79
crystal-space versus reciprocal-space
short distance long distance
long distance short distance

## Slide 80
Krivoglaz: the spatial dependence of strain: (r)

## Slide 81
0 dimensional: point defects
point-defect-type, e.g. precipitates
inclusions
(r)  1/r2
Diffraction pattern: diffuse scattering

## Slide 82
1 dimensional: dislocations
non-equilibrium triple-junctions
linear-type defects
(r)  1/r
Diffraction pattern: line broadening

## Slide 83
2 dimensional: planar defects, e.g. stacking faults
twin boundaries
grain boundaries
domain boundaries
(r)  constant
Diffraction pattern: peak shift

## Slide 84
Line broadening is caused by strain: if and only if
strain is produced by linear-type defects
the prototype of which are: dislocations

## Slide 85
Fundamental equation for line-broadening: Warren [1958]:
Dislocation-model for <g,L2>: Wilkens [1970]:
b : Burgers vector
 : dislocation density
C : Contrast factor of dislocations
f() : Wilkens function [1970]
 = L/Re
AL(g)  ALS exp{ - 22L2g2 <g2> }
Strain Fourier coefficients
= f()

## Slide 86
The Wilkens function [1970]
f ()
~ 1/
~ ln()

## Slide 87
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
T
Dislocation arrangement parameter
random highly correlated
Re > d 1/2=1/d
M = Re/d = Re1/2 > 1
Re<< d 1/2=1/d
M = Re1/2 << 1
d
d
Re
Re

## Slide 89
Strain profile 3 parameters (in cubic crystals)
dislocation - density : 
- arrangement parameter: M
contrast factor - strain anisotropy: q

## Slide 90
Strain profile:
inverse Fourier transform of the strain Fourier coefficients
ID(s) = exp{ - 22L2g2 <L,g2> }exp(2iLs)dL
where:

## Slide 91
Size profile: IS
assuming log-normal size distribution:
m: median
: variance

## Slide 92
CMWP method
Philosophy of evaluation
IMeas < = > IStrain*ISize*Iplanar defects * IInstr + BG
Non-linear, least squares fitting
IStrain : , M, q M = Re 1/2
ISize : m, 
Iplanas defects :  or 
In cubic crystals altogether: 5+1 parameters
Physically modeled
Experimentally determined
Measured pattern

## Slide 93
CdF2 ball milled for 12 min
G. Ribárik, N. Audebrand, H. Palancher, T. Ungár and D. Louër, J. Appl. Cryst. (2005). 38, 912–926

## Slide 94
Thank you
for your
attention